**S1 Table**

|  |  |  |
| --- | --- | --- |
| **Element** | **Atomic %**  **(Result)** | **Method** |
| C | 50.51 | GLI Procedure ME-12 |
| H | 6.68 | GLI Procedure ME-12 |
| Ga | 9.05 | GLI Procedure ME-70 |
| N | 7.08 | GLI Procedure ME-12 |